## Slide 1: Information on AIE’s data analysis / simulation / optimization side
Timothy Yap, 04/23/2026

## Slide 2: Agenda
Broadly, how does VPP work
Setting up a simulation for VPP (2D at first), and comparing to experimental results
Setting up the optimization
Future work

## Slide 3: Broadly, how does VPP work

## Slide 4: Jacobs (1992), at UT’s 1st SFF Symposium
‘SLA’ is described via the movement of a (Gaussian-distribution) laser on top of resin
The working curve is important:
x-axis = time * intensity (called “exposure”/ “dose”/ “dosage”)
y-axis = Cure Depth
Questions:
Is dosage always reciprocal?
How do you measure ‘degree of cure’ anyway, other than cure depth (which is only analogous)?
Beer-Lambert attenuation into the resin?
What happens below critical dose 6.8 mJ/cm2?

## Slide 5: Q1: Reciprocal? or non-linear?
Dosage = I × t
But some people started noticing nonlinearities in the working curve (Wyden 2014, Rudenko 2024), but Uzcategui 2018 put it together and proposed an exponent ‘n’: i.e., Dosage = In × t
n = 0.68

## Slide 6: Where does non-linearity come from?
Multi-step chemistries, so perhaps some later stage creates inhibitors, accelerators [sic]
  Uzcategui: “While primary photochemical reactions such as absorbance and initiator cleavage follow the first order scaling of reciprocity, radical polymerizations are known for their sub-linear dependence on light intensity due to subsequent bimolecular radical termination…”
  Crucially, pre-knowledge of the multiple steps is not needed
Multiple wavelengths which may act as …
  Crucially, pre-knowledge of full spectra response is not needed

## Slide 7: Where does non-linearity come from?
Stevens 2023 (Page group) also cite oxygen inhibition, optical self-focusing, optical scattering, heating (exotherms or from external light sources), photobleaching (resin turns from translucent to transparent after curing, allowing deeper conversions)
  They investigate multiple wavelengths for conversion (only for LEDs), and their solution is to use a Recker-Jacobs equation which accounts for differential absorption

## Slide 8: Let’s be clear on how they measured time
Uzcategui: not stated
Stevens: in a rheometer, starting from when they start the light
I suspect there is human error in starting a stopwatch, but what do I know

## Slide 9: Implications
Will the n exponent capture all the secondary / higher-order effects?
  Namely, exotherms, optical scattering / self-focusing / photobleaching, oxygen…
Conclusion: I don’t care, let’s just simulate it

## Slide 10: Q2: We want to use ‘degree of cure’
Working curve’s ‘cure depth’ is only analogous to ‘degree of cure’ (DoC) / ‘degree of conversion’ / ‘conversion’
Let’s first be clear on how they measured depth
Bennett 2017: stylus profilometry uses a small force, but will not work well on the sides of the part. Confocal is good for that. Calipers are fine for rigid materials.

## Slide 11: How they measured DoC: FTIR
FTIR shoots IR onto / into a sample
  It comes back / goes through, and has to interfere with itself such that you can see the interference
  The Fourier Transform will use the interference to break down the wavenumbers (cm-1) absorbed: requiring chemistry pre-knowledge
Question: do they state which mode?
  Transmission mode: goes through the entire thing
    Question: if transmission, how thick? 1um? 1km?
  Attenuated Total Reflection / Specular Reflection: just the surface
    Question: if surface, like, 1um into the surface? 1nm?

## Slide 12: How they measured DoC: FTIR
Uzcategui 2018 (mode?) use real-time FTIR to measure acrylate monomer conversion.
Stevens 2023 fig 3ab: it doesn’t go to full?
  Wydra (??), Mason, Kiker (100umTRANS) also not full
  Page 2024 (50 or 100umTRANS), Gao 2024 (??) yes full
  So do you care that it goes to 100% conversion?

## Slide 13: How they measured DoC
Schroeder: Absorbance spectra
  Create various samples, arrested at 5s, 10s, 15s, etc.
  Shine the entire IR – Vis – UV range, see which absorbances change
  I guess we rely on the fact (hope) that absorbance spectra change at all
Hoppe: Raman instead
About half of them don’t even measure DoC! E.g. Caplins, Rudenko, Li, Rau, Shusteff
Other methods? Atomic Force Microscopy, bulk rheology, bulk tensile/compressive testing?

## Slide 14: Conclusion on DoC
Frankly, the only pixel-by-pixel data that we can get, in real time, is: AIE
  AIE is when you shine a UV light, it fluoresces red light out
  We can use a physical narrowband filter on the camera to grab the red light (with some tiny spillover of the UV light)
  Note: AIE is known to start fluorescing when it’s already partially cured
  Units = red light videoframe intensity (0~255 or 0~65535)
We will henceforth only use AIE results, and disregard all other results

## Slide 15: Q3: unit area or unit volume?
VPP is 3D, but assumes each layer requires some intensity that is applied throughout that layer
We know that using Beer-Lambert law, light will attenuate (like sunlight propagating through seawater onto the seabed)
Blah blah, I don’t care until we set up the 3D

## Slide 16: Q4: what happens before critical dose?
Bowman (UC Boulder), Taki (Kanazawa) groups check ALL chemical equations
Photo-Radicals● have a choice to either 2a. convert/polymerize or 2b. turn into peroxides (eat oxygen)
  At least two papers suggest that 2a. occurs at a rate “two or more orders of magnitude” faster than 2b.
I.e. that 6.8mJ/cm2 wait time is just to eat up all oxygen
1. Photo-initiation
2a. Conversion / polymerization
2b. Oxygen-eating

## Slide 17: Q4: how we will model this
Calculate light incident per pixel
3. Any leftover light just goes to waste
Next timestep
1. Radicals try to convert oxygen
Radicals
O2
2. Any leftover radicals try to increase cure
Cure
Cure
O2
t
t
Radicals

## Slide 18: Q5: Diffusion
Zak’s original idea was to model oxygen diffusion, and the assumption is that it causes blur
2 ways to model oxygen:
  Fick’s Laws
≤½ per Courant’s FEA Law :- if you violate this, it goes negative, it doesn’t make physical sense, and would be unstable.
Or ≤¼ if in 2D
me
my right neighbor
my left neighbor
Due to the extremely small timesteps needed to fulfil Courant’s Law, this approach is NOT favored

## Slide 19: Diffusion
2nd way to model oxygen: Gaussian convolutions, favored by Orth and the Swiss
https://en.wikipedia.org/wiki/Kernel_(image_processing)#Convolution
It gives the exact same results (to 8-bit accuracy) while running 10x faster

## Slide 20: Diffusion
Any other diffusion? Photoradicals, photoinitiators, monomers
  Much larger molecules, so technically the effects will be much smaller
  So technically these are facilitators, in the sense that if a pixel has zero light, it’s possible for it to still cure if the neighbors have light.
  We define oxygen as inhibitive diffusion, in the sense that if a pixel has light, it’s possible for it to NOT cure if the neighbors have zero light.
  Hence, the inhibitive effect should be bigger than the facilitative effect
  I.e., the effect for external corners is much bigger than internal corners (e.g., in an L-shape)

## Slide 21: “Diffusion”
Any other contributors to blur?
Yes, light easily scatters / diverges during propagation through air, through the air-resin interface, etc.
We model it simply as a Gaussian kernel convolution (again)
  For light, we blur light ONCE per simulation.
  For oxygen, we blur oxygen every time step in each simulation.
This results in both facilitative and inhibitive effects

## Slide 22: Setting up a simulation for VPP (2D at first), and comparing to experimental results

## Slide 23: Model setup
1. Radicals try to convert oxygen
Radicals
O2
2. Any leftover radicals try to increase cure
Cure
Light scattering
Oxygen is diffused by Fick’s Laws
Chemical model in each pixel
Import original shape as the projected image
Next time-step
Cure
O2
t
t
Assume light = radicals
Radicals

## Slide 24: All required constants (for bulk curing)
O2
DoC
Dosage
Notes:
We change x-axis to ‘dosage’, assuming each timestep will receive the same amount of light
The DoC curve must come from AIE fluorescence units (0~255), nothing else
We have to disregard blurring effects, simply by asking Xiaofeng to do AIE videos on big circles, and we analyze only the middle of the circle (far away from diffusing edges)
Required constants:
What is the downslope of the O2 = ‘LtoeatO2’ ?
  It’s linear (same timesteps = same dosage = same O2 conversion)
  We don’t assume reciprocity, i.e., the downslope is a function dependent on intensity
What is the ‘upslope’ of the DoC?
  Firstly, shape is DoC for t > 0, per some papers. We first fit the exponent = 1, 2, etc. This number is tied to the particular resin.
  Secondly, fit K2 as a function of intensity.
I.e., get Xiaofeng to give us big-circle videos for various intensities, then we fit LtoeatO2 and K2 as a function of intensity

## Slide 25: Bulk curing video example
Fitting C & D, ignore A & B which depend on camera
Repeat for all videos
A
B
16-bit grayscale
C
D
Fit
Chart: Dosage C for 0mM_329
| 10 | 10 | 15 | 15 | 20 | 20 | 25 | 25
 | 17.2377 | 16.6514 | 17.1761 | 17.2402 | 21.7144 | 20.5386 | 19.2636 | 20.0957

## Slide 26: All required constants (for diffusive effects)
As before, get Xiaofeng to take some L-shape videos
  Experimentally, we find that all blurring effects, when eyeballed to simulation results, give a very large error bar
  Also, we find facilitative blurring effects ~ inhibitive, meaning, chemical effects are near zero. Most blurring comes from light scattering
  Experimentally, she’s done two intensities: blurring doesn’t change a lot
Example experimental, t=2.8s
Simulation if kernel size is: 300um 500um 600um

## Slide 27: Note for her videos
Technically, it’s fluorescence. Meaning, if no UV, then no red light
  Which means, whenever we are interested in timestep t=?, we will STOP the UV light at that timestep, and then do a big blast of UV across the ENTIRE SETUP.
Note: any time the setup / resin changes, ask her to redo all videos

## Slide 28: What are we really checking? ‘Blur’?
Zak asks for a better metric for comparing two images (experimental/simulation or experimental/experimental, etc.)
  Peak signal-to-noise ratio, PSNR, MATLAB app / Python app from Jack
  Contrast , favored by Rajesh Menon, but it is more sensitive to weak than strong
Zak + Xiaofeng ask for a better metric on ‘blur’
  Note: This is NOT a comparison
  Variance of Laplacian (see MATLAB code)
  Width of blur (draw a line across the boundary of interest, see MATLAB code)

## Slide 29: Setting up the optimization

## Slide 30: Machine learning to find minimum
x
How to find minimum, i.e., vary x until you get desired y?
Human way = trivial
Machine way, if we know the function:
Choose any one starting point
Calculate gradient
Take a small step rightwards to go downwards
Reach another point
Calculate gradient
Take a small step rightwards to go downwards
Reach another point
Calculate gradient
Take a small step rightwards to go downwards
…
Gradient is 0 = no further improvement
y
1,2,3
4,5,6
7,8,9
10
Caveats that we are not interested in:
Local minima
‘Small’er step = reduce learning rate ‘lr’

## Slide 31: Machine learning as applied to us: x
The toy example only varies one x to find minimum y.
We can have multiple x-axes
  Gradient is described in terms of x1, x2, …
  Direction to move is therefore described in the same x1, x2, …
So obviously, we can vary all 300×300 pixels = we can vary 90,000 x-variables
y
x1
x2

## Slide 32: Machine learning as applied to us: y
Can we have multiple y axes? NO, instead:
y = Σ(cure-target)2 for all pixels, this is our ‘loss’
Think of loss as ‘wrong’ness:
  If cure is 1 but target is 0, then wrongness = (1)2 = 1
  If cure is 0 but target is 1, then wrongness = (-1)2 = 1
  If cure is 1 and target is 1, then wrongness = 0
  If cure is 0.5 and target is 1, then wrongness = 0.25
  …
  Hence sum up all the wrongness for the y

## Slide 33: Machine learning as applied to us: y
Technically, in the loss, we have to specify the timestep
If we specify an intensity of 25mW/cm2 and the target shape at t=1s, then the optimizer probably fails (duh)
  So choose a reasonable timestep please
Choose multiple timesteps? Why not? Sum up each loss
  We can target zero cure at t=13s, partial cure at t=16s, full cure at t=19s
All this is easy to do by converting numpy variables to PyTorch variables

## Slide 34: Machine learning as applied to us: y
Taking a closer look: algorithm records the DoC
It requires a gradient! Zero gradient = doesn’t know where to move = optimizer stalls
O2
DoC
Dosage
O2
DoC
Dosage
We simply add a tiny upslope so the optimizer knows where to move

## Slide 35: Side question
Is there always an answer? Assume one time-step: you have 300×300 inputs and 300×300 outputs, surely you always solve it?
Deconvolutions run into high-frequency noise issues
Even so, negative intensities will result
So no
To get better results, use smaller light-scattering blur values

## Slide 36: Side note: Rackson2021
Great idea from UCB’s Hayden Taylor: process (anti-)window
  It works for CAL (not VPP exactly); no idea how to implement to us

## Slide 37: Future work

## Slide 38: Future work
Modeling TEMPO (another inhibitor) and PI diffusion?
  Relatively (?) simple to add into the simulation
3D
  The setup: take a picture of the top layer – do the bottom layers affect it?
  nth layer’s light will affect n-1th layer – Beer-Lambert
Open-loop video
  Both simulation and optimization will need tweaking
Closed-loop video
  A. is it even possible? How many frames we talking about? Computer fast?
  B. Control system